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DESCRIPTION
YHCoat-1000 is a two-component, polymer-modified cementitious waterproofing slurry designed for effective waterproofing applications. It consists of two main components: a liquid polymer emulsion blended with various additives and an inorganic powder material composed of cement and fillers. When mixed in specific proportions, these components form a waterproofing slurry that can be applied to surfaces to create a durable, robust and water-resistant coating.
WHERE TO USE
Suitable for interior applications such as toilets, bathrooms, kitchens, balconies, floors, flat roof, and floor heating systems, as well as exterior non-tile and stone facade systems for building walls. It can also be used for maintaining the waterproof layer of underground foundations.
CHARACTERISTICS AND PACKAGING
	Item
	Part A
	Part B

	Appearance
	White thick liquid
	Grey powder

	Density
	2.0 kg/L

	Mixing Ratio (in weight)
	Part A : Part B = 3 : 10 

	Packing Size
	6kg per plastic pail
	20kg per valve bag


ADVANTAGES
· Green, safe, and environmentally friendly.
· Can be directly applied to wet surfaces, offering excellent impermeability.
· Smooth application process with fast drying, saving time and labor.
· Strong adhesion to the substrate, ensuring a durable bond.
PROPERTIES
	Description
	Test Methods
	Typical Values

	Pull-Off Strength (To Concrete)
	ASTM D7234
	≥ 1.0 Mpa

	Compressive Strength
	ASTM C109/ 109M
	≥ 14 Mpa

	Flexural Strength
	ASTM C348
	≥ 7 Mpa

	Water Vapor Transmission
	BS EN ISO 12572
	≈ 1.02×10-6 kg/(s ·m²)

	Liquid Water Permeability
	BS EN 1062-3
	≈ 0.057 kg/m².h0.5 (Class W3 )

	Permeability to Carbon Dioxide
	BS EN 1062-6
	≈ 0.29 g/(m².d)

	Resistance to water penetration
	DIN 1048 Pr 5
	≈ 90 mm

	Water impermeability (1.5bar, 7d)
	BS EN 14891, A7
	≈ 0 mm


Note: The above data were tested under standard conditions (temperature 23 °C ± 2 °C, relative humidity 50% ± 10%). 

APPLICATION INSTRUCTIONS
Application Information
	Mixing ratio
	Used as slurry: A: B = 3 : 10 (by weight)

	Consumption & Coverage
	2.2-2.4kg/m², 11-12m² / set@1mm dry film

	Recommended thickness
	1.0 mm dry film by 2 coats
1.1-1.2kg/ m² /coat, For areas subject to high water ingress, apply a 3rd coat at 1.1-1.2 kg/m²

	Application temperature
	+5 °C min. / +35 °C max

	Pot life
	≈ 30 minutes (at +30°C). At higher temperatures, the pot life may be reduced.

	Minimum Over coating Waiting Time
	Waiting time between coats:
+10°C: 12hours;
+20°C: 6hours;
+30°C: 3hours


Application
Substrate Treatment
Ensure that the substrate is firm, clean, dry and free from contaminants such as dirt, oil, grease, old paint and loose materials.
Mixing
Slowly add powder composition (B) to liquid composition (A) in a clean container and mix. Use a forced mixer or perform mechanical mixing in a clean bucket with a drill and paddle. Until a homogeneous, lump-free condition is achieved. Stirring time: 3 minutes.
Application
Before waterproof application, the substrate must be fully wetted to saturation with clear water, but there shall be no visible water. Apply the mixed YHCoat-1000 in one direction with a stiff brush, roller, or broom. After the first coat is hardened, apply YHCoat-1000 for the second coat in the direction perpendicular to the first application direction.
Curing Treatment
Protective measures must be taken to avoid rapid drying when applied directly under sunlight and high wind conditions.
Tool Cleaning
All tools and application equipment shall be cleaned with water immediately after use. Hardened/cured material     can only be removed mechanically.
TRANSPORTATION AND STORAGE
· The product should be stored in a well-ventilated area, protected from sunlight, rain, frost and fire. Avoid squeezing or impact during transportation. The recommended storage temperature range is 5°C to 35°C. Under normal transportation and storage conditions, the shelf life is a minimum of 12 months.
[bookmark: _GoBack]PRECAUTIONS
· YHCoat-1000 does not provide a traffickable finish. Protect with a leveling screed.
· YHCoat-1000 is not a decorative treatment and may display signs of “blooming” after rain or in damp weather conditions. This does not affect the performance of the coating.
· Special attention is required to avoid puncturing the waterproof coating with fixings. 
· Protect freshly applied material from freezing and rain.
· This product contains alkaline substances, such as cement, which may cause skin allergies. Protective measures should be taken during use.
HEALTH AND SAFETY
Users should refer to the latest Material Safety Data Sheet (MSDS), which contains physical, ecological, toxicological, and other safety-related data, for information and advice on the safe handling, storage, and disposal of chemicals.
DISCLAIMER
The above information and recommendations which are based on our experience are as for reference, they can't replace the customers’ own experimental results. Since our company, our representatives or distributors can't control the transportation, storage, handling and use conditions of the products, the economic disputes and the quality accident caused by improper use can't be attributed to our suggest. In any application, the customer shall be responsible to comply with obligations of third-party intellectual property rights. Without our consent, anyone shall not provide technical information to third parties.
Website: www.oyhglobal.com 
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