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InfinShineTM Glass Wool Insulation Batts

	[image: ]Safety, Eco-friendliness, Sound Absorption, Light Weight


Description
Glass Wool Insulation Batts are fiberglass insulation products designed around an environmental protection concept. They prioritize high-efficiency insulation and sustainability, making them suitable for walls, roofs, celling and other areas in
residential and commercial buildings. These batts deliver solutions for building energy efficiency and green living.
Features & Benefits
[image: ]    Safe, Proven Ingredients: Meets strict safety benchmarks for consistent long-term performance.
[image: ]    Non-Combustible: Fire-resistant to prevent ignition in emergencies, boosting protection.
[image: ]    Sound-Absorbing: Dampens rain noise outdoors, reducing indoor disturbance for quietness.
[image: ]    Easy Installation: Lightweight, flexible design enables quick setup (even for non-professionals).
[image: ]    Cost-Effective: Enhances home comfort with low costs for long-term value.
[image: ]    Sustainable: Made with ≥80% recycled glass to cut landfill waste, supporting eco-practices.
[image: ]    GREENGUARD Gold Certified: Meets low-emission standards for healthier air (ideal for families, seniors, allergy sufferers).
[image: ]    Compression packaging for easier handling and reduced volume.
Uses
u Wood-framed wall, floor, and roof/ceiling cavity applications.
u Metal-framed wall and floor cavity applications.
u Interior surfaces of basement and unvented crawl space foundation walls.
Technical Data

	PROPERTY
	VALUE
	TEST METHOD

	Corrosion of Steel
	Pass
	C1617

	Non-combustibility
	Complies
	CAN/ULC-S114

	Smoulder Resistance Corrosion
	Average Mass Loss ≤ 2%, Individual Mass Loss ≤ 3%
	CAN/ULC-S129

	Surface Burning Characteristics
	Flame Spread 0; Smoke Developed 0
	CAN/ULC-S102

	Fungi Resistance
	Pass
	ASTM C1338









Specification

	THERMAL
RESISTANCE
	
APPLICATION
	
THICKNESS
	
WIDTH
	
LENGTH
	COVERAGE/
BAG

	RSI
	R
	
	
	
	
	SQ. M.
	SQ. FT.

	


2.1
	


12
	

Wood Frame
	

89 mm (3.5")
	279 mm (11")
	1219 mm (48")
	13.65
	146.7

	
	
	
	
	381 mm (15")
	1194 mm (47")
	9.1
	97.9

	
	
	
	
	
	1219 mm (48")
	9.29
	100

	
	
	
	
	584 mm (23")
	1194 mm (47")
	13.95
	150.1

	
	
	
	
	
	1219 mm (48")
	14.24
	153.3

	
	
	Steel Frame
	92 mm (3.625")
	406 mm (16")
	1219 mm (48")
	9.91
	106.7

	
	
	
	
	610 mm (24")
	1219 mm (48")
	14.86
	160

	
2.4
	14
	Wood Frame
	89 mm (3.5")
	381 mm (15")
	1194 mm (47")
	7.28
	78.3

	
	
	
	
	584 mm (23")
	1194 mm (47")
	11.16
	120.1

	
	
	Steel Frame
	92 mm (3.625")
	413 mm (16.25")
	1219 mm (48")
	8.05
	86.7

	3.5
	20
	Steel Frame
	152 mm (6")
	406 mm (16")
	1219 mm (48")
	7.93
	85.3

	
	
	
	
	610 mm (24")
	1219 mm (48")
	11.89
	128

	3.9
	22
	Wood Frame
	140 mm (5.5")
	381 mm (15")
	1194 mm (47")
	4.55
	49

	
	
	
	
	584 mm (23")
	1194 mm (47")
	6.97
	75.1

	
4.2
	24
	Wood Frame
	140 mm (5.5")
	375 mm (14.75")
	1194 mm (47")
	3.13
	33.7

	
	
	
	
	578 mm (22.75")
	1194 mm (47")
	4.83
	52

	
	
	Steel Frame
	152 mm (6")
	413 mm (16.25")
	1219 mm (48")
	3.52
	37.9

	

4.9
	

28
	Unrestricted
Cavity
	216 mm (8.5")
	381 mm (15")
	1219 mm (48")
	4.64
	50

	
	
	
	
	406 mm (16")
	1219 mm (48")
	4.95
	53.3

	
	
	
	
	610 mm (24")
	1219 mm (48")
	7.43
	80

	
	
	Cavity
Restricted
	178 mm (7")
	381 mm (15")
	1219 mm (48")
	2.79
	30

	
	
	
	
	584 mm (23")
	1219 mm (48")
	4.27
	46

	
Certifications and Sustainable Features
GREENGUARD GOLD Certified products are certified to GREENGUARD standards for low chemical emissions into indoor air during product usage.

[bookmark: _GoBack][image: ]

	
In fin shine
	

Shanghai Infinshine New Materials Technology Co., Ltd.
Room 108, Building 1, No. 5158 Jinshan Avenue, Jinshan District, Shanghai, China
Postal Code: 201500
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