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InfinshineTM Mineral Wool SF16 & SF24
Soundproofing and Fire Insulation

Description
[image: ]Mineral Wool SF16 & SF24 are a
premium semi-rigid stone wool batt
insulation for exterior wood/steel stud assemblies in new builds and
renovations. Its innovative flexible
edges compress during installation,
then spring back to seal studs and fill
wall cavities fully—ensuring easy fitting and consistent rated R-value.
Non-combustible with strong fire resistance, it retains integrity under direct flame, emits no toxic smoke,   and stops flame spread (meeting strict fire standards). It also resists water/moisture (preventing mold) and offers excellent sound absorbency for better indoor acoustics.
A high-performance choice for home energy efficiency, it cuts wall heat transfer to lower HVAC loads. GREENGUARD and ULC certified, it supports healthier, safer interiors.

Features & Benefits
[image: ]    Non-combustible & Fire-resistant: Mineral Wool SF16 & SF24 generate no smoke and suppresses flame spread when exposed to fire.
[image: ]    Effortless Installation: Featuring a proprietary flexible-edge design, simply insert SF Mineral Wool batt into the stud cavity, compress, and release for a secure fit.
[image: ]    Superior Noise Reduction & Sound Absorption: Effectively mitigates noise and absorbs sound, helping create quieter, more productive environments.
[image: ]    Water & Moisture Resistant: Mineral Wool inhibits mold growth, ensuring long-term performance in humid conditions.




Uses
u Engineered specifically for framed exterior wall cavities.
u Precision-sized for compatibility with both wood and steel stud construction.
u Versatile application suitable for attic floors and cathedral ceilings.
u Optimal solution for basement renovation projects.


Technical Data

	Item
	Performance
	Test
Standard

	

Reaction to
Fire
	[image: ][image: ]Flame spread rating (FSR)=15,
Smoke developed classification (SDC)=5

Class A
	
CAN/ULC S
102

	
	
	GB/T 8624

	Density
	≥1.94lbs/ft3  (≥30kg/m3)
	ASTM C167

	Corrosion
Resistance
	Corrosiveness to Steel-Passed
	ASTM C665
GB/T 11835

	
Reaction to
Moisture
	[image: ]Mass Moisture Absorption Rate (50℃,95% RH, 96H) ≤0.5%
Hydrophobicity Rate ≥98%
	GBT 5480

	
	
	GBT10299

	Asbestos
Phase
	Asbestos-Free
	HJ/T206

	Dimension
	47" x 15.25" x 3"  (1194mm X 387mm X 76mm),12pcs/bag 47" x 23" x 3" (1194mm X 584mm X 76mm), 8pcs/bag
	

	Acoustical
Performance
	Thickness
	(In.)        3
	125Hz
0.19
	250Hz
0.83
	500Hz
1.2
	1000Hz
1.14
	2000Hz
1.04
	4000Hz
1.09
	NRC
ASTM C423
1.05



Certifications and Sustainable Features
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Shanghai Infinshine New Material Technology Co., Ltd.
Room 108, Building 1, No. 5158 Jinshan Avenue, Jinshan District, Shanghai, China
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